# Solar shading system
DUCO Ventilation & Sun Control
DucoSun Wing 600

## Description

Permanent external shading system made of aluminium with movable blades. The DucoSun Wing is perforated and thus assures perfect harmony between solar shading and shadow. The large wing-shaped blade provides an urban design and, in addition to the standard perforation, is also available in other perforations on request.

The blades are mounted on site in the supporting structure (horizontally or vertically). The blades are continuously adjustable thanks to the linear electric drive motor.

## Version

### Blade

- Blade type		Wing 600

- Shape of blade	wing

- Blade height		600 mm

- Blade width		115 mm

- Perforation		Ø 10 mm, other perforations on request

- Inclination angle	0° to 90°, continuously adjustable

### Mullion

- 60/100, fixing directly to the supporting structure

### Motor

- Power supply		230 VAC, 50 Hz

- Current		0.55 A

- Electric power		126 W

- IP class		IP65

- Cable length		2 m from actuator

### Accessories

- Aluminum stop for mullion 60/100 available

## Material and surface treatment

### Blade

- Aluminium		AlMg3

Profile thickness: min. 1 mm

- Finish

  - Natural anodised (15-20 μm) according to Qualanod

  - Polyester powder coated (60-80 μm) according to Qualicoat Seaside type A (specific RAL codes or textured paint on request)

### Mullion

- Aluminium		EN AW-6063 T66 (EN 573-3)

Profile thickness: min. 3 mm

- Finish

  - Natural anodised (15-20 μm) according to Qualanod

  - Polyester powder coated (60-80 μm) according to Qualicoat Seaside type A (specific RAL codes or textured paint on request)

### Coverplate

- Aluminium		AlMg3

Lasered, 5 mm thick

- Finish

  - Natural anodised (15-20 μm) according to Qualanod

  - Polyester powder coated (60-80 μm) according to Qualicoat Seaside type A (specific RAL codes or textured paint on request)

## Technical specifications

### Strength calculation

According to EN 1990, EN 1991, EN 1999